## Slide 1
Controlling surface morphology of electrodeposited gold for the preparation of electrochemical aptasensors
@
Department of Chemistry & Biochemistry
Nanostructured Macroscale EAB Sensors
Conclusions and Future Work
Electrochemical, Aptamer-Based Sensing
Danté N. Comer, Olivia Stuehr, Amanda Ritz, Robert A. Lazenby
Acknowledgements
FSU Startup Funds
References
1Trasatti, S.; Petrii, O. A. Pure Appl. Chem. 1991, 63 (5), 711−734.
2Liu, Y.; Canoura, J.; Alkhamis, O.; Xiao, Y. ACS Appl. Mater. Interfaces 2021, 13 (8), 9491–9499.
References
Text
Introduction
https://www2.chem.fsu.edu/~lazenby/
Lab website:
Nanostructured Microscale EAB Sensors
Conclusions:
Target-assisted decreases sensing performance on the microscale.
Enhancing the ECSA decreases sensing performance on the macroscale and increases performance on the microscale.
Future work:
Microscale: Test operational stability of microelectrode EAB sensors and acquire more data for the detection of target molecules that vary in size.
Macroscale: Fabricate sensors for large molecule targets such as thrombin to verify sensing trends.
Schematic of target analyte detection
Why EAB Sensing?
Reagentless
Reversible analytical detection
Highly specific
Gives rapid results in real time
Electrodeposited Au nanostructures on microelectrodes enhances S/N.
Surface area enhancement via constant potential electrodeposition.
Aptamer-only vs Aptamer-target complex EAB sensor immobilization
Effects of electrodeposition on EAB sensor performance
unmodified
nanostructured
Ket < K’et
Ket
K’et
Constant potential electrodeposition of Au nanostructures to control morphology.
Applying a potential of -0.2 V to gold electrodes for 120 s (B) and 600 s (C) in a solution of 10 mM HAuCl4/0.5 M H2SO4 gave rise to unique surface characteristics. (A) depicts an unmodified electrode. (D) depicts the i-t curve, which results from the nucleation and growth processes of Au nanostructures on the electrode surface.
0 s
120 s
600 s
0 s
120 s
600 s
Components of an EAB sensor
EAB sensor performance dependent on electrodeposition conditions for both target analytes tested..
Kd=1000 µM
LOD=7.48 µM
Langmuir isotherm calibration curve for quantifying sensor performance
Optical image of 120 s deposited ME
The Aptamer-target immobilization2 method led to a lower aptamer packing density, and decreased signal changes observed on the microscale. This decrease in signal change contradicts the trend reported in the literature2.
EAB sensor titration of ATP with traditional aptamer-only incubation.
EAB sensor titration of ATP with fabricated with aptamer-target complex
Enhancing the ECSA increased the aptamer packing density and ATP signal change for microscale sensors.
Square wave voltammograms (SWVs) for detecting ATP
Langmuir isotherm fit on ATP calibration curves
0 50 100 150 200 250
ECSA
Geometric
Deposition time / s
Aptamer packing density / molecules/cm2
Surface area vs Deposition time
18
16
14
12
10
8
6
4
2
0
Integrate charge (Q) from Au oxide reduction peak
ECSA (cm2) = (Q) /(400 µC∙cm-2) 1
planar
nanostructured
CV in 0.05 M H2SO4 to characterize (ECSA)
Modification of planar Au electrode
1 µm
1 µm
1 µm
1 µm
A
B
D
C
30
60
120
240
Deposition Time / s
0.5
1
1.5
2
2.5
3
3.5
4
4.5
ECSA / cm2
ECSA vs Deposition time
Charge associated with growth of nanostructures
Electrode edge
Electrode center
Deposition Time / s
Current / µA
Dopamine
ATP
Aptamer Probe Packing Density
Langmuir isotherm calibration curves for detection of target analyte
Project Goal: Use electrodeposition of gold nanostructures to control the morphology of sensors and investigate its impact on the binding affinity, aptamer packing density, and signal change of EAB sensors on the micro- and macroscale.
Aptamer packing density
Binding affinity (Kd) between aptamer and target analyte
Target analyte signal change
EAB sensor descriptors:
L
L
azenby
ab
_
What is an electrochemical, aptamer-based sensor?
Electrochemical, aptamer-based (EAB) sensors are electrochemical biosensors that utilize structure-switching aptamer probes attached to electrodes to detect analytes.
Current / µA
Charge / C
ECSA / cm2
Aptamer packing density / molecules/cm2
Deposition time / s
250
200
150
100
50
0
0
2
4
6
8
10
12
14
0
200
400
600
Dopamine Concentration / µM
0
50
100
150
200
250
Signal Change / %
0
500
1000
1500
2000
2500
ATP Concentration / µM
0
20
40
60
80
100
120
Signal Change / %
0 s Kd = 833 µM
120 s Kd = 1099 µM
600 s Kd = 1664 µM
0 s Kd = 22.32 µM
120 s Kd = 33.78 µM
600 s Kd = 68.49 µM
6-mercaptohexanol
(backfilling molecule)
Nucleic acid oligomer
Leucomethylene blue
(redox-active molecule)
Sensor Interrogation Methods:
Kd = 1000 µM
Kd = 192 µM
30 s
60 s
120 s
S, Smax = peak current
[L] = target concentration
Langmuir isotherm parameters
Apparent binding affinity Kd between target analyte and aptamer
Au electrode surface
25 µM